- Tujuan/Objective

Untuk memastikan tata cara pemeriksaan bahan baku Hydroxypropyl Cellulose (Klucel LF) dilakukan dengan baik dan benar sesuai spesifikasi yang berlaku.

To guarantee that the method for testing Hydroxypropyl Cellulose (Klucel LF) raw materials is followed appropriately and in accordance with applicable requirements.

- Ruang Lingkup/Scope

Laboratorium PT. Kimia Farma, Tbk. - Plant Banjaran

PT. Kimia Farma, Tbk. - Plant Banjaran Laboratory

- Penanggung Jawab/Responsibility

Analis Pengawasan Mutu bertanggung jawab melaksanakan pemeriksaan bahan baku Hydroxypropyl Cellulose (Klucel LF) sesuai dengan instruksi kerja ini.

The Quality Control Analyst responsible for inspecting Hydroxypropyl Cellulose (Klucel LF) raw materials in accordance with the working instruction.

- Definisi/Definition

-

- Referensi/Reference

USP 43, NF 38

- Alat dan Bahan/Equipments and Materials

  - Alat/Equipments :

| 1. | Botol Timbang/Weighing Bottle | 16. | Pipet Tetes/Drop Pipette |
| --- | --- | --- | --- |
| 2. | Buret/Burette | 17. | Pipet Ukur/Measuring Pipette |
| 3. | Cawan Pijar/Crucible | 18. | Spektrofotometer IR |
| 4. | Desikator/Desiccator | 19. | Timbangan Analitik/Analytical Balance |
| 5. | Furnace | 20. | Viskometer/Viscometer |
| 6. | Gelas Kimia/Beaker Glass | 21. | Lumpang dan Alu/Mortar dan Pestle |
| 7. | Gelas Ukur/Measuring Cylinder | 22. | Gas Chromatography (GC) |
| 8. | Hot Plate | 23. | Kolom GC: DB-624 30 m x 0,53 mm; 3 µm GC Column: DB-624 30 m x 0.53 mm; 3 µm |
| 9. | Inductively Coupled Plasma (ICP) | 24. | Mikropipet/Micropipette |
| 10. | Kaca Arloji/Watch Glass | 25. | Pipet Seukuran/Volumetric pipette |
| 11. | Labu Ukur/Volumetric Glass | 26. | Reaction Vial |
| 12. | Magnetic Stirrer | 27. | Syringe |
| 13. | Oven Vakum/Vacuum Pump | 28. | Tip Mikropipet/Micropipette Tips |
| 14. | Penjepit Cawan/Crucible Tong | 29. | Vial GC/GC vials |
| 15. | pH meter | 30. | Waterbath |

  - Bahan/Materials :

| 1. | Air Murni/Purified Water | 8. | ICP Multi-element Standard Solution IV 100 ppm |
| --- | --- | --- | --- |
| 2. | Asam Sulfat P/Sulfuric Acid | 9. | Asam Nitrat P/Nitric Acid |
| 3. | Kalium Bromida P Dried Potassium Bromide | 10. | Baku Kerja Hydroxypropyl Cellulose (Klucel LF) Hydroxypropul Cellulose (Klucel LF) Working Standard |
| 4. | Hydrogen Floride P | 11. | Air bebas CO2/Carbon dixode-free water |
| 5. | Adipic Acid | 12. | Methylcyclohexane |
| 6. | Hydroiodic Acid | 13. | Mineral Oil |
| 7. | Isopropyl Iodide | 14. | o-xylene |

- Instruksi Kerja/Work Instruction

  - Pemerian (R)/Description (R)

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

Amati secara visual (Organoleptik).

Visually observe (Organoleptic).

  - Identifikasi (R)/Identification (R)

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Serapan Inframerah/Infrared Absorption

- Zat Baku/Standard Substance

- Campur dan gerus 8 mg baku kerja Hydroxypropyl Cellulose (Klucel LF) dengan 400 mg Kalium Bromida kering.

Mix and grind 8 mg of Hydroxypropyl Cellulose (Klucel LF) working standard with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Buat pellet Kalium Bromida.

Make Potassium Bromide pellets.

- Zat Uji/Sample Substance

- Campur dan gerus 8 mg zat uji Hydroxypropyl Cellulose (Klucel LF) dengan 400 mg Kalium Bromida kering.

Mix and grind 8 mg of Hydroxypropyl Cellulose (Klucel LF) sample with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Buat pellet Kalium Bromida.

Make Potassium Bromide pellets.

- Pengukuran/Measurement

- Lakukan “scanning” menggunakan spektrofotometer IR pada panjang gelombang 400 - 4000 nm.

Use an IR spectrophotometer to do "scanning" at a wavelength of 400 - 4000 nm.

- Bandingkan spektra zat uji dengan zat baku.

Compare the spectra of the test substance with the standard substance.

- Amati kedua spektra tersebut, spektrum serapan inframerah zat uji menunjukkan maksimum hanya pada panjang gelombang yang sama seperti pada zat baku.

Observe the two spectra, the infrared absorption spectrum of the test substance shows a maximum only at the same wavelength as the standard substance.

- Reaksi Kimia/Chemical Reaction

- Timbang 1 gram zat uji, masukkan ke dalam gelas kimia.

Weigh 1 gram of the sample substance, put it in a beaker glass.

- Larutkan dalam 100 ml Air Murni.

Dissolve in 100 mL of Purified Water.

- Pipet 1 ml larutan tersebut ke atas sebuah kaca arloji, lalu uapkan.

Pipette 1 mL of the solution onto a watch glass and vaporize.

- Amati/Observe.

  - Sisa Pemijaran/Residue of Ignition

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Pijarkan cawan pijar platina pada suhu 600 ± 50oC di dalam Furnace, selama 30 menit.

Incandescent crucible at a temperature of 600 ± 50oC in the Furnace, for 30 minutes.

- Dinginkan cawan pijar platina dalam desikator dan timbang (Wo).

Cool the crucible in a desiccator before weighing it (Wo).

- Timbang seksama 1-2 g zat uji ke dalam cawan pijar platina (Wa).

Weigh accurately 1-2 g of sample substance, put into crucible (Wa).

- Tambahkan 1 ml Asam Sulfat P.

Add 1 mL of concentrated Sulfuric Acid.

- Panaskan sampai zat uji mengarang sempurna, lalu dinginkan.

Heat until sample substance is carbonized perfectly, then allow to cool.

- Basahi residu dengan 1 ml Asam Sulfat P.

Moisten the residue using 1 mL of concentrated Sulfuric Acid.

- Panaskan lagi hingga uap putih hilang.

Reheat until the white haze has gone.

- Pijarkan dalam Furnace pada suhu 600 ± 50oC hingga arang habis terbakar.

Incandescent in the Furnace at a temperature of 600 ± 50 oC until the charcoal burns out.

- Dinginkan cawan pijar platina dalam desikator, timbang saksama (Wb).

Allow crucible to cool in desiccators, weigh carefully (Wb).

- Jika jumlah residu yang diperoleh melebihi batas yang ditetapkan, basahi lagi residu dengan 1 ml Asam Sulfat P.

If the amount of residue obtained exceeds the specified limit, moisten the residue again with 1 mL of Sulfuric Acid P.

- Panaskan lagi hingga uap putih hilang.

Reheat until the white haze has gone.

- Pijarkan dalam Furnace pada suhu 600 ± 50oC selama 30 menit.

Incandescent in the Furnace at a temperature of 600 ± 50 oC for 30 minutes.

- Dinginkan cawan pijar platina dalam desikator, timbang saksama (Wb).

Allow crucible to cool in desiccators, weigh carefully (Wb).

    - Perhitungan/Calculation :

SPn= Wb-WoWa-Wo × 100%

Keterangan/Note :

SPn	= 	Sisa pemijaran (%)

Residue of ignition (%)

Wo	= 	Berat cawan pijar kosong (gram)

Weight of empty crucible (grams)

Wa	= 	Berat cawan pijar + zat uji sebelum pemijaran (gram)

Weight of crucible + sample substance before ignition (grams)

Wb	= 	Berat cawan pijar + zat uji setelah pemijaran (gram)

Weight of crucible + sample substance after ignition (grams)

  - Silika/Silica

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Tambahkan beberapa tetes Air Murni pada residu yang diperoleh pada pemeriksaan Sisa Pemijaran.

Add a few drops of Purified Water to the residue obtained on the Residu on Ignition Examination.

- Tambahkan secara perlahan 5 ml HF.

Slowly add 5 mL of HF.

- Uapkan di atas Hotplate hingga hampir kering, lalu dinginkan.

Evaporate on a hotplate until almost dry, then allow to cool.

- Tambahkan 5 ml HF dan 0,5 ml Asam Sulfat P, kemudian uapkan hingga hamper kering.

Add 5 mL of HF and 0.5 mL of sulfuric acid P, then evaporate until almost dry.

- Secara perlahan, naikkan suhu Hotplate hingga seluruh asam menguap.

Slowly raise the hotplate temperature until all the acid has evaporated.

- Pijarkan di dalam Furnace, pada suhu 1000oC.

Incandescent in the Furnace, at a temperature of 1000oC.

- Dinginkan cawan pijar dalam desikator, timbang saksama (Wb).

Allow crucible to cool in desiccators, weigh carefully (Wb).

    - Perhitungan/Calculation :

%Silica= Wsi-WoWa-Wo × 100%

Keterangan/Note :

| %Silica | = | Kadar Silica (%) Silica Content (%) |
| --- | --- | --- |
| Wo | = | Berat cawan pijar kosong pada pemeriksaan Sisa Pemijaran (gram) The weight of the empty crucible in the Residue on Ignition Examination (grams) |
| Wa | = | Berat cawan pijar + zat uji sebelum pemijaran pada pemeriksaan Sisa Pemijaran (gram) Weight of crucible + sample substance before ignition in the Residue on Ignition Examination (gram) |

  - Timbal/Lead

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Persiapan Larutan/Solution Preparation

- Larutan Asam Nitrat 2,5%/2.5% Nitric Acid Solution

      - Ambil 500 ml Air Murni, masukkan ke dalam gelas kimia 1000 ml.

Fill a 1000 mL beaker glass halfway with 500 mL of Purified Water.

- Tambahkan 38,5 ml Asam Nitrat P secara perlahan; aduk hingga homogen.

Add 38.5 mL of Nitric Acid P slowly; stir until homogeneous.

- Tambahkan 461,5 ml Air Murni;  aduk hingga homogen.

Add 461.5 mL of Purified Water; stir until homogeneous.

- Larutan Baku Multi-element Induk/Multi-element Standard Solution

- Pipet 2 ml ICP Multi-element Standard Solution IV 100 ppm, masukkan ke dalam labu ukur 20 ml.

Pipette 2 mL ICP Multi-element Standard Solution IV 100 ppm, put into a 20 ml volumetric flask.

- Tambahkan larutan Asam Nitrat 2,5% hingga tanda batas volume; kocok hingga homogen.

Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Saring menggunakan syringe filter 0,2 µm.

Filter using a 0.2 µm syringe filter.

(Konsentrasi Pb: 10 ppm)/(Concentration of Pb: 10 ppm)

- Larutan Baku Multi-element 0,1 ppm/Multi-element Standard Solution 0.1 ppm

- Pipet 0,5 ml Larutan Baku Multi-element Induk; masukkan ke dalam labu ukur 50 ml.

Pipette 0.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Tambahkan larutan Asam Nitrat 2,5% hingga tanda batas volume; kocok hingga homogen.

Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Saring menggunakan syringe filter 0,2 µm.

Filter using a 0.2 µm syringe filter.

(Konsentrasi Pb: 0,1 ppm)/(Concentration of Pb: 0.1 ppm)

- Larutan Baku Multi-element 0,3 ppm/Multi-element Standard Solution 0.3 ppm

- Pipet 1,5 ml Larutan Baku Multi-element Induk; masukkan ke dalam labu ukur 50 ml.

Pipette 1.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Tambahkan larutan Asam Nitrat 2,5% hingga tanda batas volume; kocok hingga homogen.

Add 2.5% Nitric Acid solution to volume; and shake until homogenous.

- Saring menggunakan syringe filter 0,2 µm.

Filter using a 0.2 µm syringe filter.

(Konsentrasi Pb: 0,3 ppm)/(Concentration of Pb: 0.3 ppm)

- Larutan Baku Multi-element 0,5 ppm/Multi-element Standard Solution 0.5 ppm

- Pipet 2,5 ml Larutan Baku Multi-element Induk; masukkan ke dalam labu ukur 50 ml.

Pipette 2.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Tambahkan larutan Asam Nitrat 2,5% hingga tanda batas volume; kocok hingga homogen.

Add 2.5% Nitric Acid solution to volume; and shake until homogenous.

- Saring menggunakan syringe filter 0,2 µm.

Filter using a 0.2 µm syringe filter.

(Konsentrasi Pb: 0,5 ppm)/(Concentration of Pb: 0.5 ppm)

- Larutan Uji/Sample Solution

- Timbang 2 g zat uji, masukkan ke dalam labu ukur 20 ml.

Weigh 2 g of the sample substance, put it in a 20 mL volumetric flask.

- Tambahkan larutan Asam Nitrat 2,5%; sonikasi hingga larut.

Add 2.5% nitric acid solution; sonicate until dissolved.

- Tambahkan larutan Asam Nitrat 2,5% hingga tanda batas volume; kocok hingga homogen.

Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Saring filtrat menggunakan syringe filter 0,2 µm.

Filter the filtrate using a 0.2 µm syringe filter.

- Pengukuran/Measurement

Lakukan pemeriksaan sesuai dengan Instruksi Kerja Pengoperasian Alat Inductively Coupled Plasma.

Follow the Inductively Coupled Plasma Equipment Work Instructions when performing inspections.

  - pH

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Taburkan secara perlahan 1,0 gram zat uji ke dalam gelas kimia yang berisi 100 ml air bebas CO2 mendidih.

Slowly sprinkle 1.0 gram of the test substance into a beaker glass containing 100 mL of boiling carbon dioxide-free water.

- Aduk menggunakan Magnetic Stirer sampai larut, lalu biarkan dingin hingga suhu ruang.

Stir using a Magnetic Stirer until dissolved, then let it cool to room temperature.

- Lakukan pemeriksaan sesuai dengan Instruksi Kerja Pengoperasian Alat pH Meter.

Perform checks in accordance with the pH Meter Operation Work Instructions.

  - Susut Pengeringan (R)/Loss on Drying (R)

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Panaskan botol timbang pada suhu 105 ± 2oC di dalam Oven Vakum, selama 30 menit.

Heat the weighing bottle at a temperature of 105 ± 2oC in the Vacuum Oven, for 30 minutes.

- Dinginkan botol timbang dalam desikator dan timbang seksama (Wo).

Allow to cool the weighing bottle in a desiccator and weigh thoroughly (Wo).

- Timbang seksama 20 kapsul, masukkan ke dalam botol timbang yang telah ditimbang (Wa).

Weigh carefully 1 - 2 g of the test substance, put it in a weighing bottle that has been weighed (Wa).

- Masukkan ke dalam Oven Vakum dengan suhu 105 ± 2oC.

Put it in a vacuum oven with a temperature of 105 ± 2oC.

- Keringkan selama 4 jam dalam keadaan vakum.

Dry for 4 hours in a vacuum.

- Dinginkan botol timbang dalam desikator 5 - 15 menit, timbang (Wb).

Allow to cool weighing bottle in a desiccator for 5-15 minutes before weighing (Wb).

    - Perhitungan/Calculation :

SP= Wa-WbWa-Wo × 100%

Keterangan :

SP	= 	Susut pengeringan (%)

Loss on Drying (%)

Wa	= 	Berat botol timbang + zat uji sebelum pengeringan (gram)

Weight of weighing bottle + sample substance before drying (grams)

Wb	= 	Berat botol timbang + zat uji setelah pengeringan (gram)

Weight of weighing bottle + sample substance after drying (grams)

Wo	= 	Berat botol timbang kosong (gram)

Weight of empty weighing bottle (grams)

  - Viskositas (R)/Viscosity (R)

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Timbang 10 g zat uji, masukkan sedikit demi sedikit ke dalam gelas kimia berisi 200 ml Air Murni.

Weigh 10 g of the test substance, put it little by little into a beaker containing 200 mL of Purified Water.

- Aduk hingga homogen.

Stir until homogeneous.

- Lakukan pemeriksaan kekentalan sesuai Instruksi Kerja Pengoperasian Alat Viskometer Spindel, dengan ketentuan sebagai berikut:

Perform a viscosity examination according to the Spindle Viscometer Operation Work Instructions, with the following conditions:

Suhu/Temperature	:	25°C

Spindel/Spindle	:	MS-DIN 19

Shear Rate	:	10 s-1

Waktu/Weight	: 	120 detik/120 second

  - Gugus Hydroxypropoxy (R)/Hydroxypropoxy Groups (R)

    - Syarat/Requirement :

Sesuai dengan spesifikasi Bahan Baku Hydroxypropyl Cellulose (Klucel LF) (S-QC-01-282).

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Cara Kerja/Procedure :

- Sistem Kromatografi Gas/Gas Chromatographic System:

Metoda/Methode	:	GC-Direct Inject

Kolom/Column	:	DB-624 30 m x 0,53 mm; 3 µm

Gas Pembawa/Carrier Gas	:	Helium

Average Velocity	:	5,2 cm/s (constant linear velocity)

Split Ratio	:	50:1

Detektor/Detector	:	FID

Volume Penyuntikan/Injection Volume	:	2 µl

Suhu Detektor/Detector Temperature	:	280°C

Suhu Injektor/Injector Temperature	:	180°C

Suhu Kolom/Column Temperature	:	Gradient

| Kenaikan Suhu/Temperature Increase (°C/menit) | Suhu/Temperature (°C) | Holding Time (menit) |
| --- | --- | --- |
| - | 40 | 3 |
| 10 | 100 | 0 |
| 50 | 250 | 3 |

- Blangko/Blank

Gunakan o-xylene sebagai blanko/Use o-xylene as a blank.

- Larutan Internal Standar/Insternal Standard Solution

- Pipet 1 ml Methylcyclohexane, masukkan ke dalam labu ukur 50 ml.

Pipette 1 mL of Methylcyclohexane, put it into a 50 mL volumetric flask.

- Encerkan dengan o-xylene hingga tanda batas volume, kocok hingga homogen.

Dilute with o-xylene to volume, shake until homogeneous.

- Larutan Standar/Standard Solution

- Timbang 60 mg Adipic Acid, masukkan ke dalam Reaction Vial.

Weigh 60 mg of Adipic Acid, put it in the Reaction Vial.

- Tambahkan 2000 µl Larutan Internal Standar dan 1,0 ml Hydroiodic Acid.

Add 2000 µL Standard Internal Solution and 1.0 mL Hydroiodic Acid.

- Tutup Reaction Vial tersebut, kemudian timbang (Wso).

Close the Reaction Vial, then weigh (Wso).

- Injek 25 µl Isopropyl Iodide ke dalam Reaction Vial tersebut dengan menggunakan syringe, kocok hingga homogen.

Inject 25 µL Isopropyl Iodide into the Reaction Vial using a syringe, shake until homogeneous.

- Kemudian timbang kembali Reaction Vial tersebut (Wsb).

Then weigh again the Reaction Vial (Wsb).

- Hitung selisih Wsb dan Wso sebagai bobot dari Isopropyl Iodide.

Calculate the difference between Wsb and Wso as the weight of Isopropyl Iodide.

- Setelah terpisah menjadi 2 fasa, ambil fasa atas dengan menggunakan syringe yang telah didinginkan. Kemudian masukkan ke dalam Vial GC.

After separating into 2 phases, take the upper phase using a cooled syringe. Then put it in the GC Vial.

- Larutan Uji/Sample Solution

- Timbang 30 mg zat uji (Wu) yang telah dikeringkan dan 60 mg Adipic Acid, masukkan ke dalam Reaction Vial.

Weigh 30 mg of the dried sample substance and 60 mg of Adipic Acid, put it in the Reaction Vial.

- Tambahkan 2000 µl Larutan Internal Standar dan 1,0 ml Hydroiodic Acid.

Add 2000 µL Standard Internal Solution and 1.0 mL Hydroiodic Acid.

- Tutup Reaction Vial tersebut, kemudian timbang (Wuo).

Close the Reaction Vial, then weigh (Wuo).

- Panaskan Reaction Vial tersebut pada suhu 115°C selama 70 menit sambil dilakukan pengadukan yang berkelanjutan.

Heat the Reaction Vial at 115°C for 70 minutes while continuously stirring.

- Dinginkan Reaction Vial tersebut, kemudian timbang (Wub).

Cool the Reaction Vial, then weigh (Wub).

- Jika selisih penimbangan Wub dan Wuo lebih dari 10 mg, maka lakukan preparasi ulang.

If the difference in weighing Wub and Wuo is more than 10 mg, then do the preparation again.

- Setelah terpisah menjadi 2 fasa, ambil fasa atas dengan menggunakan syringe yang telah didinginkan. Kemudian masukkan ke dalam Vial GC.

After separating into 2 phases, take the upper phase using a cooled syringe. Then put it in the GC Vial.

- Kriteria Penerimaan Uji Kesesuaian Sistem/Acceptance Criteria for System Suitability Test

| Parameter | Acceptance Criteria |
| --- | --- |
| Resolusi Resolution | Resolusi antara puncak Isopropyl Iodide dan Methylcyclohexane > 2 Resolution between Isopropyl Iodide and Methylcyclohexane peaks > 2 |
| %RSD | %RSD puncak larutan standar < 10,0% %RSD peak of standard solutions < 10.0% |

- Perhitungan/Calculation:

Faktor Respon/Response Factor:

F= LA1 × (Wsb -Wso)LA2 × 100 × B%

Keterangan/Note:

F	=	Faktor Respon

Response Factor

LA1	=	Luas area Methylcyclohexane dalam larutan standar

Peak area of Methylcyclohexane in standard solution

Wsb	=	Berat  Reaction Vial + Isopropyl Iodide (mg)

Weight of Reaction Vial + Isopropyl Iodide (mg)

Wso	=	Berat  Reaction Vial (mg)

Weight of Reaction Vial (mg)

LA2	=	Luas area Isopropy Iodide dalam larutan standar

Peak area of Isopropy Iodide in standard solution

B	=	Kadar Isopropy Iodide (%)

Content of Isopropy Iodide (%)

Gugus Hydroxypropoxy (R)/Hydroxypropoxy Groups:

GH= LA4 × F× 75,1 × 1,15LA3 × Wu × 170,0 × 100%

Keterangan :

GH	=	Gugus Hydroxypropoxy (%)

Hydroxypropoxy Groups (%)

LA4	=	Luas area Isopropy Iodide dalam larutan uji

Peak area of Isopropy Iodide in sample solution

F	=	Faktor Respon yang dihitung di atas

Response Factor calculated from above

75,1	=	Massa Molar Gugus Hydroxypropoxy

Mollar Mass of Hydroxypropoxy Groups

1,15	=	Faktor koreksi untuk mengkorelasikan hasil dengan metode pengujian sebelumnya diganti dengan metode ini

Correction factor to correlate results to previous assay methode replaced by this methode

LA3	=	Luas area Methylcyclohexane dalam larutan uji

Peak area of the Methylcyclohexane in sample solution

Wu	=	Berat zat uji kering yang ditimbang (mg)

Weight of the sample (dried substance) in the sample solution (mg)

170,0	=	Massa Molar Isopropy Iodide

Mollar Mass of Isopropyl Iodide

- Daftar Lampiran/List of Attachment

| Lampiran (Attachments) | Kode Dokumen (Document No.) | Judul Dokumen (Document Title) | Tanggal Efektif (Effective Date) |
| --- | --- | --- | --- |
| - | - | - | - |

- Sejarah Revisi dan Review/Revision and Review History

| Kode Dokumen (Document Code) | Revisi (Revision) | Tanggal Efektif (Effective Date) | Perubahan (Changes) | Alasan (Reasons) |
| --- | --- | --- | --- | --- |
| I-QC-01-282 | 00 |  | - | Dokumen Baru New Document |
| I-QC-01-282 | 01 |  | - Penambahan : Gas Chromatography (GC); Kolom GC: DB-624 30 m x 0,53 mm; 3 µm; Mikropipet, Pipet Seukuran; Reaction Vial; Syringe; Tip Mikropipet; Vial GC; Waterbath; Adipic Acid; Hydroiodic Acid; Isopropyl Iodide; Methylcyclohexane; Mineral Oil; o-xylene. - Penambahan parameter Residual Solvent: Gugus Hydroxypropoxy | Penambahan parameter Residual Solvent: Gugus Hydroxypropoxy |

- Daftar Distribusi Dokumen/Distribution List of Document

Asli/Original : SSDR

Controlled Copy :

- AMPM

- SPBB