- Objective

To guarantee that the method for inspecting Microcrystalline Cellulose pH 101 raw materials is followed appropriately and in accordance with applicable specifications.

- Scope

PT.  Kimia Farma, Tbk. - Plant Banjaran Laboratory

- Responsibility

The Quality Control Analyst is in charge of inspecting Microcrystalline Cellulose pH 101 raw materials in line with the job instructions.

- Definition

-

- Reference

USP 46 NF 41 (2023)

PT. Kimia Farma

- Equipments and Materials

  - Equipments

| 1. | Analytical Balance | 17. | pH Meter |
| --- | --- | --- | --- |
| 2. | Beaker Glass | 18. | Desiccator |
| 3. | Spektrophotometer IR | 19. | Crucible |
| 4. | Oven | 20. | Furnace |
| 5. | Conical Flask | 21. | Evaporating Dish |
| 6. | Drop Pipette | 22. | Weighing Bottle |
| 7. | Measuring Cylinder | 23. | Whatman Filter Paper No. 42 |
| 8. | Bulk Density Tester | 24. | Watch Glass |
| 9. | Sieve Shaker | 25. | Conductivity Meter |
| 10. | Centrifuge | 26. | Hot Plate |
| 11. | Magnetic Stirrer | 27. | Shaker |
| 12. | Mortar and Pestle | 28. | Crucible Tong |
| 13. | Mesh No. 60 | 29. | Waterbath |
| 14. | Mesh No. 200 | 30. | Conical Flask |
| 15. | Microscope | 31. | Thermometer |
| 16. | 100 and 150 Cannon-Fenske | 32 | Chromatographic Kolom |

  - Materials

| 1. | Purified Water | 8. | Iodine |
| --- | --- | --- | --- |
| 2. | Microcrystalline Cellulose pH 101 working standard | 9. | Zinc Chloride |
| 3. | 1 N Hydrochloric Acid | 10. | Sulfuric Acid |
| 4. | Potassium Iodide | 11. | Ethanol |
| 5. | Sodium Hydroxide Solution (1 in 20) | 12. | Dried Potassium Bromide |
| 6. | Cupriethylenediamine Hydroxide | 13. | Nitrogen Gas |
| 7. | Peroxide-free Ether | 14. | Silica |

- Work Instruction

  - Description

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

      - Organoleptis

Visually observe (Organoleptic).

      - Extraneous object

- Look for extraneous object in the sample and collect them.

- Follow the Microscope Equipment Work Instructions when performing inspections.

  - Solubility

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Solubility in water

- Dissolve 10 mg of sample with 100 mL of purified water.

- Observe the description of the solution.

- Solubility in NaOH Solution (1 in 20)

- Dissolve 10 mg of sample with 100 mL of NaOH Solution (1 in 20).

- Observe the description of the solution.

- Solubility in organic solvent

- Dissolve 10 mg of sample with 100 mL of ethanol.

- Observe the description of the solution.

- Solubility in Dilute Acids

- Dissolve 10 mg of sample with 100 mL of 1 N HCl.

- Observe the description of the solution.

  - Identification

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Infrared Absorption

- Standard Substance

- Mix and grind 8 mg of Microcrystalline Cellulose pH 101 working standard with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Make Potassium Bromide pellets.

- Sample Substance

- Mix and grind 8 mg of Microcrystalline Cellulose pH 101 sample with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Make Potassium Bromide pellets.

- Measurement

- Use an IR spectrophotometer to do "scanning" at a wavelength of 400 - 4000 nm.

- Compare the spectra of the sample substance  with the standard substance.

- Observe the two spectra, the infrared absorption spectrum of the sample substance  shows a maximum only at the same wavelength as the standard substance.

- Chemical Reaction

- Iodinated Zinc Chloride Solution

- Weigh 20 g of Zinc chloride and 6.5 g Potassium iodide into beaker glass.

- Dissolve with 10.5 mL of purified water.

- Add 0.5 g Iodine and shake for 15 minutes.

- Inspection

- Weigh 10 mg of the test substance, place it on a watch glass.

- Disperse in 2 mL Iodinated Zinc Chloride Solution.

- Observe viasually.

- Degree of Polymerization

      - Inspection

- Weigh 1.3g of sample; put into a 250 ml Conical Flask.

- Add 25 mL of water and 25 mL of 1.0 M Cupriethylenediamine Hydroxide Solution.

- Immediately, purge the solution with Nitrogen Gas.

- Close with stopper and shake on a shaker until completely dissolved.

- Add an appropriate volume of the sample solution to a calibrated 150 Cannon Fenske.

- Allow the solution equilibrate at 25±0.1°C for not less than 5 min.

- Record the flow time between 2 marks on the viscometer in second (t).

- Calculate the kinematic Viscosity of sample (KV1).

- Do the same measurement to 0.5 M Cupriethylenediamine Solution with a calibrated 100 Cannon Fenske. Calculate the kinematic Viscosity of the solution (KV2).

- Calculation :

Kinematic Viscosity

KV1	= t1 x k1

KV2	= t2 x k2

Relative Viscosity

ηrel   = (KV1)(KV2)

Degree of Polymerization

P   = (95 x ηC )WU x 100 -SP100    x 100

Keterangan:

KV1		= Kinematic Viscosity of Sample (Kv1)

KV2		= Kinematic Viscosity of 0.5 M Cupriethylenediamine Solution (KV2).

T1		= Flow time of sample (s)

T2		= Flow Time of 0.5 M Cupriethylenediamine Solution (s)

K1		= Viscometer Constant of sample

ηrel

K2		= Viscometer Constant of 0.5 M Cupriethylenediamine Solution

ηc

= Viscosity Relative

= Intrinsic Viscosity in Reference Tables Section

SP		= Loss on Drying

P			= Degree of Polymerization

  - Residue of ignition

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Incandescent crucible at a temperature of 600 ± 50oC in the Furnace, for 30 minutes.

- Cool the crucible in a desiccator before weighing it (Wo).

- Weigh 1 - 2 g of sample, put it in a taraised crucible (Wa).

- Add 1 mL of concentrated sulfuric acid.

- Heat until sample substance is totally.

- Cool, than add 1 mL of concentrated sulfuric acid.

- Reheat until the white steam has dissipated.

- Until the charcoal burns away, incandescent in a furnace at a temperature of 600oC ± 50oC.

- Allow to cool in desiccator for 5 – 15 minutes, then weigh (Wb).

- If the amount of residue obtained exceeds the specified limit, moisten the residue again with 1 mL of Sulfuric Acid P.

- Reheat until the white steam has dissipated.

- Incandescent in a furnace at a temperature of 600 ± 50 oC for 30 minutes.

- Allow to cool in desiccator 5 – 15 minutes, then weigh (Wb).

    - Calculation :

SPn= Wb-WoWa-Wo × 100%

Note :

SPn	= 	Residue of ignition (%)

Wa	= 	Weight of crucible + sample substance before ignition (grams)

Wb	= 	Weight of crucible + sample substance after ignition (grams)

Wo	= 	Weight of empty crucible (grams)

  - Conductivity

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Weigh 5 g of the sample substance, put it in a 250 mL conical flask.

- Add 40 mL of Purified Water.

- Shake using a shaker for 20 minutes.

- Centrifugation of the solution for 10 minutes at a speed of 2500 rpm, collect the supernatant.

- Follow the Conductivity Meter Equipment Work Instruction when inspecting conductivity of supernatant solution.

  - pH

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Use supernatant obtained in the conductivity test.

- Follow the pH Meter Equipment Work Instructions when performing inspections.

  - Loss on drying

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Heat the weighing bottle at a temperature of 105oC in the Oven, for 30 minutes.

- Allow to cool the weighing bottle in a desiccator for 5 – 15 minutes and weigh thoroughly (Wo).

- If the sample substance  is big crystals, mill it quickly to a particle size of ± 2 mm.

- Weigh carefully 1 - 2 g of sample, put it in a weighing bottle that has been weighed (Wa).

- Flatten the sample in the weighing bottle ± 5 mm – 10 mm.

- Put it in the oven at 105oC.

- Dry for 3 hours.

- Allow to cool in a desiccator for 5 - 15 minutes , then weighing (Wb).

    - Calculation :

SP= Wa-WbWa-Wo × 100%

Note :

SP	= 	Loss on drying (%)

Wa	= 	Weight of weighing bottle + sample before drying (grams)

Wb	= 	Weight of weighing bottle + sample after drying (grams)

Wo	= 	Weight of empty weighing bottle (grams)

  - Bulk Density

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Weigh 2 g of sample, put into beaker glass.

- Measure the volume of sample that fills the measuring cylinder (untapped density).

- Continue the inspection for tapping by Follow the Work Instructions for Bulk Density Tester.

- Measure the volume of sample after tapping (tapped density).

    - Calculation:

Keterangan:

BD   = Bulk Density (g/ml)

Wu  = Weight of sample substance (g)

Vu   = Volume of sample substance (ml)

  - Particle Size Distribution

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Take Mesh No. 60 and No. 200.

- Follow the Sieve Shaker Equipment Work Instructions when performing inspections.

    - Calculation:

Wse = Wa - Wo

Pass the Mesh = Wu - Wse Wu x 100%

Restrained by Mesh =  Wse Wu x 100%

Keterangan:

Wa		= Weight of Mesh + sample substance after screening (gram)

Wo		= Weight of empty Mesh (gram)

Wu	= Weight of sample substance being weighed (gram)

Wse		= weight of the test substance retained by Mesh (gram)

  - Water-Soluble Substances

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Weigh 5 g of sample (Wu), put into 250 mL conical flask.

- Add 80 mL of purified water, shake for 10 minutes using shaker.

- Filter the solution through Whatman No. 42 filter paper.

- Heat the evaporating dish at a temperature of 105oC in the Oven, for 30 minutes.

- Allow to cool the evaporating dish in a desiccator for 5 – 15 minutes and weigh thoroughly (Wo).

- Collect the filtrate in a evaporating dish of knowing weight.

- Evaporate on water bath until dry.

- Dry in the oven at 105oC for 1 hour.

- Allow to cool in a desiccator for 5 – 15 minutes, then weight (Wb).

    - Calculation :

ZLA = Wb -WoWu ×  100%

Keterangan:

ZLA	=	Water-Soluble Substances (%)

Wu	=	Weight of the sample substance weighed (grams)

Wb	= 	Weight of evaporating dish + residue (grams)

Wo	= 	Weight of empty evaporating dish (grams)

  - Eter-Soluble Substances

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

- Prepare the apparatus of Chromatographic Kolom.

- Attach cotton as high as 5 cm as the bottom layer of the chromatography column.

- Add silica about a half of the Kolom.

- Wet silica with Peroxide-free Ether (Diethyl Ether) Solution. Remove excess solution.

- Heat the two evaporating dish at a temperature of 105oC in the Oven, for 30 minutes.

- Allow to cool the evaporating dish in a desiccator for 5 – 15 minutes and weigh thoroughly.

- Add 50 mL of Peroxide-free Eter (Diethyl Eter) Solution to Chromatographic Kolom.

- Collect the filtrate to a evaporating dish (A1).

- Put 10 g of sample to Chromatographic Kolom.

- Add 50 mL of Peroxide-free Eter (Diethyl Eter) Solution to Chromatographic Kolom.

- Collect the filtrate to a evaporating dish (B1).

- Let the filtrate evaporate with a current of air in a fumehood.

- After all the Eter has evaporated, dry residu in a oven at 105°C for 30 min.

- Cool in a desiccator, and weigh (A2 dan B2).

    - Calculation :

ZLE = (B2-B1-A2-A1)Wu ×  100%

Keterangan:

ZLE	=	Eter-Soluble Substances (%)

Wu	=	Weight of the sample substance weighed (grams)

A1	= 	Weight of empty evaporating dish (grams)

A2	= 	Weight of evaporating dish + residue (grams)

B1	= 	Weight of empty evaporating dish (grams)

B2	=	Weight of evaporating dish + residue (grams)

  - Microbial Enumeration Test

    - Requirement :

Microcrystalline Cellulose pH 101 Raw Material specifications are met a requirement (S-QC-01-102).

    - Procedure :

Follow the Microbial Enumeration Tests procedure when performing inspections.

  - List of Attachment

| Attachments | Document Code | Document Title | Effective Date |
| --- | --- | --- | --- |
| - | - | - | - |

  - Revision and Review History

| Document Code | Revision | Effective Date | Changes | Reasons |
| --- | --- | --- | --- | --- |
| I-QC-01-101(E) | 00 |  | - | New Document |

  - Distribution List of Document

Original : SSDR

Controlled Copy :

- AMPM

- SPBB