- Objective

To show specific description of Microcyrstalline Cellulose PH 101 raw material to be used as a reference on inspection of the material.

- Scope

Explain the raw material Microcrystalline Cellulose PH 101 spesifications used in the production process at PT. Kimia Farma Tbk. Banjaran Plant.

- Material Specification

Synonyms			: Avicel pH 101

Molecular formula		: (C6H10O5)n ; n = 220

Molecular weight	 : 36.000 gram/mol

Material code			: 32000179; 32000324

| No |  | Inspection parameters |  | Unit |  | Acceptance criteria |  | Reference |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Description |  |  |  |  |  |  |  |
|  | Shape |  |  |  | Fine Powder |  | USP 46 NF 41 (2023) |  |
|  | Color |  |  |  | White or almost white |  | USP 46 NF 41 (2023) |  |
|  | Other characteristic |  |  |  | Free flowing and non-fibrous particles |  | USP 46 NF 41 (2023) |  |
|  | Extraneous object |  | mm |  | The size of the Extraneous object is not more than 7.0 |  | PT. Kimia Farma |  |
| 2 | Solubility |  |  |  |  |  |  |  |
|  | In water |  |  |  | Insoluble |  | USP 46 NF 41 (2023) |  |
|  | In organic solvent |  |  |  | Insoluble |  | USP 46 NF 41 (2023) |  |
|  | In NaOH Solution (1 in 20) |  |  |  | Practically insoluble |  | USP 46 NF 41 (2023) |  |
|  | In Diluted Acids |  |  |  | Insoluble |  | USP 46 NF 41 (2023) |  |
| 3 | Identification |  |  |  |  |  |  |  |
|  | Infrared Absorption |  |  |  | The infrared absorption spectrum of the sample substance shows a maximum only at the same wavelength as that of the standard substance. |  | USP 46 NF 41 (2023) |  |
|  | Chemical Reaction |  |  |  | The substance takes on a violet-blue color |  | USP 46 NF 41 (2023) |  |
|  | Degree of Polymerization |  |  |  | Not more than 350 |  | USP 46 NF 41 (2023) |  |
| 4 | Residue on Ignition |  | % |  | Not more than 0.1 |  | USP 46 NF 41 (2023) |  |
| 5 | Conductivity |  | µS/cm |  | Not more than 75 |  | USP 46 NF 41 (2023) |  |
| 6 | pH |  |  |  | 5,0 – 7,5 |  | USP 46 NF 41 (2023) |  |
| 7 | Loss on Drying |  | % |  | Not more than 7.0 |  | USP 46 NF 41 (2023) |  |
| 8 | Bulk Density |  | g/ml |  | 0,26 - 0,50 |  | USP 46 NF 41 (2023) & PT. Kimia Farma |  |
| 9 | Particle Size Distribution |  |  |  |  |  |  |  |
|  | Detained Mesh No. 60 |  | % |  | Not more than 1.0 |  | USP 46 NF 41 (2023) & PT. Kimia Farma |  |
|  | Detained Mesh No. 200 |  | % |  | Not more than 30.0 |  | USP 46 NF 41 (2023) & PT. Kimia Farma |  |
| 10 | Water-Soluble Substances |  | % |  | Not more than 0.25 (12,5 mg) |  | USP 46 NF 41 (2023) |  |
| 11 | Ether-Soluble Substances |  | % |  | Not more than 0.05 |  | USP 46 NF 41 (2023) |  |
| 12 | Microbial Limit Test and Identification Test |  |  |  |  |  |  |  |
|  | Total plate count |  | cfu/g |  | Not more than (103) 2000 |  | USP 46 NF 41 (2023) |  |
|  | Yeast and molds count |  | cfu/g |  | Not more than (102) 200 |  | USP 46 NF 41 (2023) |  |
|  | Staphylococcus aureus |  |  |  | Negative |  | USP 46 NF 41 (2023) |  |
|  | Pseudomonas aeruginosa |  |  |  | Negative |  | USP 46 NF 41 (2023) |  |
|  | Escherichia coli |  |  |  | Negative |  | USP 46 NF 41 (2023) |  |
|  | Salmonella sp. |  |  |  | Negative |  | USP 46 NF 41 (2023) |  |

- Revision and Review History

| Document Code | Revision | Effective Date | Changes | Reasons |
| --- | --- | --- | --- | --- |
| S-QC-01-102(E) | 00 |  | - | New Document |

- Distribution List of Document

Original : SSDR

Controlled Copy :

| 1. | AMPM |
| --- | --- |
| 2. | SPBB |