- Objective

To show specific description of Croscarmellose Sodium  raw material to be used as a reference on inspection of the material.

- Scope

Explain the raw material Croscarmellose Sodium  specifications used in the production process at PT. Kimia Farma Tbk. Banjaran Plant.

- Material Specification

| Synonyms : | - Ac-Disol | - CMC-Na |
| --- | --- | --- |
|  | - Sodium Carboxy Methyl Cellulose Crosslinked Form | - Carboxymethylcellulose Sodium |
|  | - Vivasol | - Primellose |
|  | - Cellogen F-3H | - Cellulose Gum |
| Molecular formula : | C28H30Na8O27 |  |
| Molecular weight : | 982,44 g/mol |  |
| Material code : | 32000123, 32000150 |  |

| No | Category | Unit | Acceptance Criteria | Reference |
| --- | --- | --- | --- | --- |
| 1 | Description |  |  |  |
|  | Shape |  | Powder | USP 46 NF 41 (2023) |
|  | Color |  | White | USP 46 NF 41 (2023) |
|  | Other Characteristic |  | Free-flowing | USP 46 NF 41 (2023) |
| 2 | Solubility |  |  |  |
|  | In Water |  | Partially Soluble | USP 46 NF 41 (2023) |
|  | In Ethanol |  | Insoluble | USP 46 NF 41 (2023) |
|  | In Eter |  | Insoluble | USP 46 NF 41 (2023) |
|  | In Methanol |  | Insoluble | USP 46 NF 41 (2023) |
|  | In Aceton |  | Insoluble | USP 46 NF 41 (2023) |
|  | In Chloroform |  | Insoluble | USP 46 NF 41 (2023) |
| 3 | Identification |  |  |  |
|  | Infrared identification test |  | The infrared absorption spectrum of the test substance shows a maximum only at the same wavelength as the standard substance. | USP 46 NF 41 (2023) |
|  | Identification test B |  | Absorbs the methylene blue and settles as a blue, fibrous mass | USP 46 NF 41 (2023) |
|  | Identification test C |  | A dense precipitate is formed | USP 46 NF 41 (2023) |
| 4 | # Residue on Ignition | % | #### 14,0 – 28,0 | USP 46 NF 41 (2023) |
| 5 | # The sum of Sodium chloride and Sodium glycolate | % | #### Not more than 0.5 | USP 46 NF 41 (2023) |
| 6 | Content of Water-Soluble Material | % | Not more than 10.0 | USP 46 NF 41 (2023) |
| 7 | Degree of substitution, calculated on the anhydrous basis |  | 0,60 – 0,85 | USP 46 NF 41 (2023) |
| 8 | Loss on Drying | % | Not more than 10.0 | USP 46 NF 41 (2023) |
| 9 | pH |  | 5,0 - 7,0 | USP 46 NF 41 (2023) |
| 10 | Settling Volume | mL | 10,0 - 30,0 | USP 46 NF 41 (2023) |
| 11 | # Microbial Limit Test |  |  | USP 46 NF 41 (2023) |
|  | # Total Aerobic Microbial Count | cfu/g | ### Not more than (103) 2000 | USP 46 NF 41 (2023) |
|  | # Total Combined Molds and Yeasts Count | cfu/g | ### Not more than (102) 200 | USP 46 NF 41 (2023) |
|  | # E. coli |  | Negative | USP 46 NF 41 (2023) |

- Revision and Review History

| Document Code | Revision | Effective Date | Changes | Reasons |
| --- | --- | --- | --- | --- |
| S-QC-01-128(E) | 00 |  | - | New Document |

- Distribution List of Document

Original : SSDR

Controlled Copy :

| 1. | AMPM |  |  |
| --- | --- | --- | --- |
| 2. | SPBB |  |  |