- Objective

To show specific description of Hydroxypropyl Cellulose (Klucel LF) raw material to be used as a reference on inspection of the material.

- Scope

Explain the raw material Hydroxypropyl Cellulose (Klucel LF) specifications used in the production process at PT. Kimia Farma Tbk. - Banjaran Plant.

- Material Specification

| Synonyms | : | - Cellulose | - Nisso HPC |
| --- | --- | --- | --- |
|  |  | - 2-Hydroxypropyl Ether | - Hydroxypropyl Eter |
|  |  | - Oxypropylated Cellulose | - Hyprolose |
| Molecular formula | : | - |  |
| Molecular weight | : | - |  |
| Material code | : | 32001072 |  |

| No | Category | Unit | Acceptance Criteria | Reference |
| --- | --- | --- | --- | --- |
| 1 | Description |  |  |  |
|  | Shape |  | Powder | USP 46 NF 41 (2023) |
|  | Color |  | White or almost white | USP 46 NF 41 (2023) |
| 2 | Identification |  |  |  |
|  | Infrared Absorption |  | The infrared absorption spectrum of the sample substance shows a maximum only at the same wavelength as that of the standard substance. | USP 46 NF 41 (2023) |
|  | Chemical Reaction |  | A thin film is formed | USP 46 NF 41 (2023) |
| 3 | # Residue on Ignition | % | #### Not more than 0.8 | USP 46 NF 41 (2023) |
| 4 | Silica | % | Not more than 0.6 | USP 46 NF 41 (2023) |
| 5 | Lead | ppm | Not more than 10 | Modification USP 46 NF 41 (2023) |
| 6 | pH |  | 5,0 - 8,0 | USP 46 NF 41 (2023) |
| 7 | Loss on Drying | % | Not more than 5.0 | USP 46 NF 41 (2023) |
| 8 | Viscosity | cps | ### 75 - 150 | USP 46 NF 41 (2023) and PT. Kimia Farma |
| 9 | Hydroxypropoxy Groups | % | ### 53,4 – 80,5 | USP 46 NF 41 (2023) |
| 10 | Microbial Enumeration Tests |  |  |  |
|  | The Total Aerobic Microbial Count | cfu/g | ### Not lower than 103 (2,000) | USP 46 NF 41 (2023) |
|  | # The Total Combined Molds and Yeasts Count | cfu/g | ### Not lower than 102 (200) | USP 46 NF 41 (2023) |

- Revision and Review History

| Document Code | Revision | Effective Date | Changes | Reasons |
| --- | --- | --- | --- | --- |
| S-QC-01-282(E) | 00 |  | - | New Document |

- Distribution List of Document

Original : SSDR

Controlled Copy :

- AMPM

- SPBB