- Objective

To guarantee that the method for testing Hydroxypropyl Cellulose (Klucel LF) raw materials is followed appropriately and in accordance with applicable requirements.

- Scope

PT. Kimia Farma, Tbk. - Plant Banjaran Laboratory

- Responsibility

The Quality Control Analyst responsible for inspecting Hydroxypropyl Cellulose (Klucel LF) raw materials in accordance with the working instruction.

- Definition

-

- Reference

Modifikasi USP 46 NF 41 (2023); PT. Kimia Farma

- Equipments and Materials

  - Equipments :

| 1. | Weighing Bottle | 16. | Drop Pipette |
| --- | --- | --- | --- |
| 2. | Burette | 17. | Measuring Pipette |
| 3. | Platinum Crucible | 18. | Spektrofotometer IR |
| 4. | Desiccator | 19. | Analytical Balance |
| 5. | Furnace | 20. | Viscometer |
| 6. | Beaker Glass | 21. | Mortar dan Pestle |
| 7. | Measuring Cylinder | 22. | Gas Chromatography (GC) |
| 8. | Hot Plate | 23. | GC Column: DB-624 30 m x 0.53 mm; 3 µm |
| 9. | Inductively Coupled Plasma (ICP) | 24. | Micropipette |
| 10. | Watch Glass | 25. | Volumetric pipette |
| 11. | Volumetric Glass | 26. | Reaction Vial |
| 12. | Magnetic Stirrer | 27. | Syringe |
| 13. | Vacuum Pump | 28. | Micropipette Tips |
| 14. | Crucible Tong | 29. | GC vials |
| 15. | pH meter | 30. | Waterbath |

  - Materials :

| 1. | Purified Water | 8. | ICP Multi-element Standard Solution IV 100 ppm |
| --- | --- | --- | --- |
| 2. | Sulfuric Acid | 9. | Nitric Acid |
| 3. | Kalium Bromida P | 10. | Baku Kerja Hydroxypropyl Cellulose (Klucel LF) |
| 4. | Hydrogen Floride P | 11. | Carbon dixode-free water |
| 5. | Adipic Acid | 12. | Methylcyclohexane |
| 6. | Hydroiodic Acid | 13. | Mineral Oil |
| 7. | Isopropyl Iodide | 14. | o-xylene |

- Work Instruction

  - Description

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

Visually observe (Organoleptic).

  - Identification

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Infrared Absorption

- Standard Substance

- Mix and grind 8 mg of Hydroxypropyl Cellulose (Klucel LF) working standard with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Make Potassium Bromide pellets.

- Sample Substance

- Mix and grind 8 mg of Hydroxypropyl Cellulose (Klucel LF) sample with 400 mg of dry Potassium Bromide in a mortar and pestle.

- Make Potassium Bromide pellets.

- Measurement

- Use an IR spectrophotometer to do "scanning" at a wavelength of 400 - 4000 nm.

- Compare the spectra of the test substance with the standard substance.

- Observe the two spectra, the infrared absorption spectrum of the test substance shows a maximum only at the same wavelength as the standard substance.

- Chemical Reaction

- Weigh 1 gram of the sample substance, put it in a beaker glass.

- Dissolve in 100 mL of Purified Water.

- Pipette 1 mL of the solution onto a watch glass and vaporize.

- Observe.

  - Residue of Ignition

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Incandescent platinum crucible at a temperature of 600oC ± 50oC in the Furnace, for 30 minutes.

- Cool the platinum crucible in a desiccator before weighing it (Wo).

- Weigh accurately 1-2 g of sample substance, put into platinum  crucible (Wa).

- Add 1 mL of concentrated Sulfuric Acid.

- Heat until sample substance is carbonized perfectly, then allow to cool.

- Moisten the residue using 1 mL of concentrated Sulfuric Acid.

- Reheat until the white haze has gone.

- Incandescent in the Furnace at a temperature of 600 oC ± 50 oC until the charcoal burns out.

- Allow platinum crucible to cool in desiccators, weigh carefully (Wb).

- If the amount of residue obtained exceeds the specified limit, moisten the residue again with 1 mL of Sulfuric Acid P.

- Reheat until the white haze has gone.

- Incandescent in the Furnace at a temperature of 600 oC ± 50 oC for 30 minutes.

- Allow platinum crucible to cool in desiccators, weigh carefully (Wb).

    - Calculation :

SPn= Wb-WoWa-Wo × 100%

Note :

SPn	= 	Residue of ignition (%)

Wo	= 	Weight of empty platinum crucible (grams)

Wa	= 	Weight of platinum crucible + sample substance before ignition (grams)

Wb	= 	Weight of platinum crucible + sample substance after ignition (grams)

  - Silica

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Add a few drops of Purified Water to the residue obtained on the Residu on Ignition Examination.

- Slowly add 5 mL of HF.

- Evaporate on a hotplate until almost dry, then allow to cool.

- Add 5 mL of HF and 0.5 mL of sulfuric acid P, then evaporate until almost dry.

- Slowly raise the hotplate temperature until all the acid has evaporated.

- Incandescent in the Furnace, at a temperature of 1000oC.

- Allow platinum crucible to cool in desiccators, weigh carefully (Wsi).

    - Calculation :

%Silica= Wsi-WoWa-Wo × 100%

Note :

| %Silica | = | Silica Content (%) |
| --- | --- | --- |
| Wo | = | The weight of the empty platinum crucible in the Residue on Ignition Examination (grams) |
| Wa | = | Weight of platinum crucible + sample substance before ignition in the Residue on Ignition Examination (gram) |

| Wsi | = | Weight of platinum crucible + sample substance after ignition in the Residue on Silica Examination (gram) |
| --- | --- | --- |

  - Lead

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Solution Preparation

- 2.5% Nitric Acid Solution

      - Fill a 1000 mL beaker glass halfway with 500 mL of Purified Water.

- Add 38.5 mL of Nitric Acid P slowly; stir until homogeneous.

- Add 461.5 mL of Purified Water; stir until homogeneous.

- Multi-element Standard Solution

- Pipette 2 mL ICP Multi-element Standard Solution IV 100 ppm, put into a 20 ml volumetric flask.

- Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Filter using a 0.2 µm syringe filter.

(Concentration of Pb: 10 ppm)

- Multi-element Standard Solution 0.1 ppm

- Pipette 0.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Filter using a 0.2 µm syringe filter.

(Concentration of Pb: 0.1 ppm)

- Multi-element Standard Solution 0.3 ppm

- Pipette 1.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Add 2.5% Nitric Acid solution to volume; and shake until homogenous.

- Filter using a 0.2 µm syringe filter.

(Concentration of Pb: 0.3 ppm)

- Multi-element Standard Solution 0.5 ppm

- Pipette 2.5 mL Multi-element Standard Solution; put into a 50 mL volumetric flask.

- Add 2.5% Nitric Acid solution to volume; and shake until homogenous.

- Filter using a 0.2 µm syringe filter.

(Concentration of Pb: 0.5 ppm)

- Sample Solution

- Weigh 2 g of the sample substance, put it in a 20 mL volumetric flask.

- Add 2.5% nitric acid solution; sonicate until dissolved.

- Add 2.5% Nitric Acid solution to volume and shake until homogenous.

- Filter the filtrate using a 0.2 µm syringe filter.

- Measurement

Follow the Inductively Coupled Plasma Equipment Work Instructions when performing inspections.

  - pH

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Slowly sprinkle 1.0 gram of the test substance into a beaker glass containing 100 mL of boiling carbon dioxide-free water.

- Stir using a Magnetic Stirer until dissolved, then let it cool to room temperature.

- Perform the examination accordance with the pH meter operation work instructions.

  - Loss on Drying

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Heat the weighing bottle at a temperature of 105 ± 2oC in the Vacuum Oven, for 30 minutes.

- Allow to cool the weighing bottle in a desiccator and weigh thoroughly (Wo).

- Weigh carefully 1 - 2 g of the test substance, put it in a weighing bottle that has been weighed (Wa).

- Put it in a vacuum oven with a temperature of 105 ± 2oC.

- Dry for 4 hours in a vacuum.

- Allow to cool weighing bottle in a desiccator for 5-15 minutes before weighing (Wb).

    - Calculation :

SP= Wa-WbWa-Wo × 100%

Keterangan :

SP	= 	Loss on Drying (%)

Wa	= 	Weight of weighing bottle + sample substance before drying (grams)

Wb	= 	Weight of weighing bottle + sample substance after drying (grams)

Wo	= 	Weight of empty weighing bottle (grams)

  - Viscosity

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Weigh 10 g of the test substance, put it little by little into a beaker containing 200 mL of Purified Water.

- Stir until homogeneous.

- Perform a viscosity examination according to the Spindle Viscometer Operation Work Instructions, with the following conditions:

Temperature	:	25°C

Spindle	:	MS-DIN 19

Shear Rate	:	10 s-1

Weight	: 	120 second

  - Hydroxypropoxy Groups

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

- Gas Chromatographic System:

Methode	:	GC-Direct Inject

Column	:	DB-624 30 m x 0,53 mm; 3 µm

Carrier Gas	:	Helium

Average Velocity	:	5,2 cm/s (constant linear velocity)

Split Ratio	:	50:1

Detector	:	FID

Injection Volume	:	2 µl

Detector Temperature	:	280°C

Injector Temperature	:	180°C

Column Temperature	:	Gradient

| Temperature Increase (°C/min) | Temperature (°C) | Holding Time (min) |
| --- | --- | --- |
| - | 40 | 3 |
| 10 | 100 | 0 |
| 50 | 250 | 3 |

- Blank

Use o-xylene as a blank.

- Internal Standard Solution

- Pipette 1 mL of Methylcyclohexane, put it into a 50 mL volumetric flask.

- Dilute with o-xylene to volume, shake until homogeneous.

- Standard Solution

- Weigh 60 mg of Adipic Acid, put it in the Reaction Vial.

- Add 2000 µL Standard Internal Solution and 1.0 mL Hydroiodic Acid.

- Close the Reaction Vial, then weigh (Wso).

- Inject 25 µL Isopropyl Iodide into the Reaction Vial using a syringe, shake until homogeneous.

- Then weigh again the Reaction Vial (Wsb).

- Calculate the difference between Wsb and Wso as the weight of Isopropyl Iodide.

- After separating into 2 phases, take the upper phase using a cooled syringe. Then put it in the GC Vial.

- Sample Solution

- Weigh 30 mg of the dried sample substance (Wu) and 60 mg of Adipic Acid, put it in the Reaction Vial.

- Add 2000 µL Standard Internal Solution and 1.0 mL Hydroiodic Acid.

- Close the Reaction Vial, then weigh (Wuo).

- Heat the Reaction Vial at 115°C for 70 minutes while continuously stirring.

- Cool the Reaction Vial, then weigh (Wub).

- If the difference in weighing Wub and Wuo is more than 10 mg, then do the preparation again.

- After separating into 2 phases, take the upper phase using a cooled syringe. Then put it in the GC Vial.

- Acceptance Criteria for System Suitability Test

| Parameter | Acceptance Criteria |
| --- | --- |
| Resolution | Resolution between Isopropyl Iodide and Methylcyclohexane peaks > 2 |
| %RSD | %RSD peak of standard solutions < 10.0% |

- Calculation:

Response Factor:

F= LA1 × (Wsb -Wso)LA2 × 100 × B%

Note:

F	=	 Response Factor

LA1	=	 Peak area of Methylcyclohexane in standard solution

Wsb	=	Weight of Reaction Vial + Isopropyl Iodide (mg)

Wso	=	Weight of Reaction Vial (mg)

LA2	=	 Peak area of Isopropy Iodide in standard solution

B	=	Content of Isopropy Iodide (%)

Hydroxypropoxy Groups:

GH= LA4 × F× 75,1 × 1,15LA3 × Wu × 170,0 × 100%

Keterangan :

GH	=	Hydroxypropoxy Groups (%)

LA4	=	Peak area of Isopropy Iodide in sample solution

F	=	Response Factor calculated from above

75,1	=	Mollar Mass of Hydroxypropoxy Groups

1,15	=	Correction factor to correlate results to previous assay methode replaced by this methode

LA3	=	Peak area of the Methylcyclohexane in sample solution

Wu	=	Weight of the sample (dried substance) in the sample solution (mg)

170,0	=	Mollar Mass of Isopropyl Iodide

  - Microbial Enumeration  Test

    - Requirement :

Hydroxypropyl Cellulose (Klucel LF) Raw Material specification are met a requirement (S-QC-01-282).

    - Procedure :

Follow the Microbial Enumeration Test Procedure when performing inspections.

  - List of Attachment

| Attachments | Document Code | Document Title | Effective Date |
| --- | --- | --- | --- |
| - | - | - | - |

  - Revision and Review History

| Document Code | Revision | Effective Date | Changes | Reasons |
| --- | --- | --- | --- | --- |
| I-QC-01-282(E) | 00 |  | - | New Document |
| I-QC-01-282(E) | 01 |  | - Add details to the silica parameter - Change in the type of equipment used | Add details to the silica parameter |

  - Distribution List of Document

Original : SSDR

Controlled Copy :

- AMPM

- SPBB

- SPML